| BRICK – PANELS JOINT ALIGNMENT SYSTEM |  |  |
| --- | --- | --- |

| XPS RIGID FOAM PANELS High Performance Insulation for our Brick-Tiles Characteristics data Joint alignment system XPS Rigid Foam WLS 035, 036,037 |  |  |  |  |  |  |  | Stand 05.2010 Date: 30.05.2010 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XPS Rigid Foam | HFC, CFC-and HCFC-free, guaranteed quality |  |  |  |  |  |  |  |  |  |  |  |
| Properties: | Non-glowing, non-melting, and is not dropping off whilst burning, Biological harmless, non-rotting, recyclable, mould and mildew-resistant. |  |  |  |  |  |  |  |  |  |  |  |
| Apparent density | >30 kg/m² in accordance with DIN EN 1602 |  |  |  |  |  |  |  |  |  |  |  |
| Compressive strength at 10% compression | >300 kPa in accordance with DIN EN 826 |  |  |  |  |  |  |  |  |  |  |  |
| Rated value of thermal conductivity | λ 0,035 W/(m-K) in accordance with DIN EN 4108-4 60 mm (CFR 300) λ 0,037 W/(m-K) in accordance with DIN EN 4108-4 80 mm (CFR 300) λ 0,036 W/(m-K) in accordance with DIN EN 4108-4 180 mm (KF 300) λ 0,037 W/(m-K) in accordance with DIN EN 4108-4 180-200 mm (KF 300) |  |  |  |  |  |  |  |  |  |  |  |
| Water vapour resistance index | 250-80 in accordance with DIN EN 12086 |  |  |  |  |  |  |  |  |  |  |  |
| Application type | WAB in accordance with DIN EN 4108-10 |  |  |  |  |  |  |  |  |  |  |  |
| Construction material class With brick tiles | B1 in accordance with DIN EN 4102 Euroclass E System can be used up to 22 meter Other high on request |  |  |  |  |  |  |  |  |  |  |  |
| Up application Temperature | +75˚C |  |  |  |  |  |  |  |  |  |  |  |
| Longitudinal expansion coefficient | 0,07 in accordance with DIN EN 1604 |  |  |  |  |  |  |  |  |  |  |  |
| Water absorption | Approx. 3 vol.% in accordance with DIN EN 12087 |  |  |  |  |  |  |  |  |  |  |  |
| Coating | no |  |  |  |  |  |  |  |  |  |  |  |
| Edge finishing | Head site stepped, sides with tongue and groove from thickness 30 mm |  |  |  |  |  |  |  |  |  |  |  |
| Dimension/Format | RF/WDF-123.0x54.5 cm NF-123.0x58.0 cm DF-123.0x56.5 cm |  |  |  |  |  |  |  |  |  |  |  |
| Thickness rigid PUR in mm U-value (W/m²-K) R-value (m²-K/W) | 16 0,50 2,00 | 25 0,71 1,40 | 30 0,85 1,25 | 40 1,14 0,87 | 60 1,71 0,58 | 80 2,16 0,46 | 100 2,77 0,36 | 120 3,33 0,30 | 140 3,88 0,25 | 160 4,44 0,23 | 180 4,86 0,21 | 200 5,40 0,19 |
| Brick –tile type/dim. In mm | NF240x71x14/17, WDF 210/215x65x14/21, RF 240x65x14/17 DF240x52x14/17, other format /thickness on request |  |  |  |  |  |  |  |  |  |  |  |
| Brick –tile colours | See website www.brick-panels.co.uk |  |  |  |  |  |  |  |  |  |  |  |
| Admission | Other technical details on request. Deutsches Institute fur Bautechnik. Berlin |  |  |  |  |  |  |  |  |  |  |  |
| Fourways ML 42 Valentines Road Ilford, ESSEX London IG1 4SA; Tel./fax: +44(0)20822271036 +44(0)7712284159 +44(0)7545966558 e.mail: info@brick-panels.co.uk www.brick-panels.co.uk. |

The above information is based on current knowledge and experience. No binding assurance in respect of certain  properties or suitability for certain applications must be read into our information. Patent rights and other proprietary rights must be observed if necessary.

Please note: As part of our continuing product development and improvement policy, we reserve the right to change product specifications without prior notice. Product colour may vary on screen so please visit the contact us page to order a copy of our product guide for more accurate colour specifications.

26.03.2013