| BRICK – PANELS DEPOSITED PANEL |  |  |
| --- | --- | --- |

| PHENOL - RIGID FOAM PANELS High Performance Insulation extra for Brick-Panels and Joint Alignment System Characteristics data Compound system and Joint alignment system Phenol-rigid foam (deposited panel) WLS 022, WLS 024 |  | Stand 06.2011 Date: 30.06.2011 |
| --- | --- | --- |
| Phenol-rigid foam | CFC-and HCFC-free, guaranteed quality |  |
| Properties: | Non-glowing, non-melting, and is not dropping off whilst burning, Biological harmless, non-rotting, recyclable, mould and mildew-resistant. |  |
| Apparent density | >35 kg/m² in accordance with DIN EN 1602 |  |
| Rated value of thermal conductivity | λ 0,022 W/(m-K) in accordance with DIN EN 4108-4, 45-120 mm λ 0,024 W/(m-K) in accordance with DIN EN 4108-4, 25-44 mm |  |
| OK | 38 in accordance with DIN EN 12086 |  |
| Application type | WAB in accordance with DIN EN 4108-10 |  |
| Construction material class Deposited rigid foam With brick tiles | B1 in accordance with DIN EN 4102 System can be used up to 22 meter Other high on request |  |
| Temperature resistance | -30˚C to +110˚C -22˚F to +230˚F |  |
| Coating | Double sided coating made of special geomembrane |  |
| Edge finishing | Around, straight |  |
| Dimension/Format | On request |  |
| General | More characteristics data on request |  |
| Fourways ML 42 Valentines Road Ilford, ESSEX London IG1 4SA; Tel./fax: +44(0)20822271036 +44(0)7712284159 +44(0)7545966558 e.mail: info@brick-panels.co.uk www.brick-panels.co.uk. |

The above information is based on current knowledge and experience. No binding assurance in respect of certain  properties or suitability for certain applications must be read into our information. Patent rights and other proprietary rights must be observed if necessary.

Please note: As part of our continuing product development and improvement policy, we reserve the right to change product specifications without prior notice. Product colour may vary on screen so please visit the contact us page to order a copy of our product guide for more accurate colour specifications.

26.03.2013